## Slide 1: Nanostructures on ultra-clean two-dimensional electron gases
T. Ihn, C. Rössler, S. Baer, K. Ensslin
C. Reichl and W. Wegscheider

## Slide 2
Electrons Clean Environment Magnetic Field
Rich variety of ground states
and excitations
Composite Fermions
J.K. Jain,
PRL 63, 199 (1989)
Willett et al,
PRL 59, 1776 (1987)
odd denominator
fractions

## Slide 3
Electrons Clean Environment Magnetic Field
Rich variety of ground states
and excitations
Willett et al,
PRL 59, 1776 (1987)
W. Pan et al,
PRL 83, 3530 (1999)
even denominator
fractions
non-abelian
anyonic excitations
topological
quantum computing
S. Das Sarma
PRL 94, 166802 (2005)
T = 8 mK
m = 17x106 cm2/Vs

## Slide 4: What we need
S. Das Sarma et al,
PRL 94, 166802 (2005)
High-mobility 2DEGs Ultralow temperatures
Tunnel Barriers Quantum Point Contacts
Quantum Dots Interferometers
utilize n=5/2 state for
topological quantum computation

## Slide 5: High Mobility 2DEGs
z (nm)
0
-100
-200
GaAs
AlGaAs
AlAs
AlAs
4 doping layers, 2 screening layers
 high mobility, but gating non-trivial
K.J. Friedland et al., PRL 77, 4616 (1996)
V. Umansky et al., J. Cryst. Growth 311, 1658 (2009)
nS
2DEG
Si
Si
Si
Si
AlGaAs
Au
screening layer
(in AlAs → Γ-band)
screening layer
(in AlAs → Γ-band)
+
+
+
+
+
+
+
+
+
+
+
+
ionized dopants
ionized dopants
C. Rössler et al., New J. Phys. 12, 043007 (2010)
Mobility µ > 107 cm2/Vs
Density nS = 3.5 x 1011 cm-2  λF = 45 nm
T = 1.9 K
B = 0.1 T
5
0
1
2
3
4
5
nS (1011 cm-2)
0
10
15
µ (106 cm2/Vs)
depletion
accumulation

## Slide 6: Quantum Point Contacts
VG1&G2(V)
5
10
15
0
G (2e2/h)
-1.2
-1.6
-2.0
QPC1: width wQPC ≈ 150-200 nm  expect 2wQPC/λF= 7-9 Subbands
Geometry: Quantum Point Contact
C. Rössler et al., New J. Phys. 13, 113006 (2011)
VG1&G2 (V)
-1.5
-2.5
-3.5
0
10
15
25
-4.5
20
5
G1
G2
200 nm
G1
G2
500 nm
G (2e2/h)
QPC2: width wQPC ≈ 450-500 nm  expect 2wQPC/λF= 20-22 Subbands
Geometry: Quantum Wire
QPC1
T = 1.3 K
VSD = 0 mV
QPC2
T = 1.3 K
VSD = 0 mV

## Slide 7: Scanning for Defects
VG1 (V)
VG2 (V)
-4
-3
-2
-1
-1
-4
-3
-2
QPC1
T = 1.3 K
0
1
0.7 × 2e2/h
2
3
Count number of plateaus  QPC shifted across 200 nm
No apparent defects (i.e. resonances) within scan range
0.7 anomaly visible throughout scan range
|dG/dVG1&G2| (a.u.)
0
1
G1
G2
200 nm
S. Schnez, C. Rössler et al., Phys. Rev. B 84, 195322 (2011)

## Slide 8: Finite Bias Transport Spectrum
VG1&G2 (V)
VSD (mV)
-12
-6
0
6
-1.3
-2.3
-2.1
-1.9
-1.7
-1.5
QPC1
T = 1.3 K
12
|dG/dVG1&G2| (a.u.)
0
1
1
2
3
1.5
2.5
3.5
4
2
3
Higher-order resonances visible
Probe subband spacings  Extract shape parameters of confinement potential
G1
G2
200 nm

## Slide 9: Finite Bias Transport Spectrum
VG1&G2 (V)
-12
-6
0
6
-1.3
-2.3
-2.1
-1.9
-1.7
-1.5
QPC1
T = 1.3 K
12
|dG/dVG1&G2| (a.u.)
0
1
1
2
3
1.5
2.5
3.5
4
2
3
Higher-order resonances visible
Probe subband spacings  Extract shape parameters of confinement potential
G1
G2
200 nm
VSD (mV)

## Slide 10: Finite Bias Transport Spectrum
VG1&G2 (V)
-12
-6
0
6
-1.3
-2.3
-2.1
-1.9
-1.7
-1.5
QPC1
T = 1.3 K
12
|dG/dVG1&G2| (a.u.)
0
1
1
2
3
1.5
2.5
3.5
4
2
3
Higher-order resonances visible
Probe subband spacings  Extract shape parameters of confinement potential
G1
G2
200 nm
VSD (mV)

## Slide 11: Lifting the Spin Degeneracy
νQPC
0
2
4
QPC3
B┴ = 2 T
VSD= 0 mV
T = 0.1 K
VG1&G2 (V)
-1.5
-2.5
-2.0
νQPC
νBULK
νBULK

## Slide 12: Lifting the Spin Degeneracy
VG1&G2 (V)
VSD (mV)
-12
-6
0
6
-1.3
-2.7
-2.5
-2.2
-1.9
-1.6
QPC3
T = 0.1 K
B┴ = 2 T
2
4
pinched
off
6
12
|dG/dVG1&G2| (a.u.)
0
1
Spin-gap enhanced by interactions: geff = -0.44 in GaAs |g*|~ 3.8 at νQPC= 5 |g*|~ 4.4 at νQPC= 3
νQPC= 1 obscured by 0.7 anomaly
3
5
νQPC
0
2
4
QPC3
B┴ = 2 T
VSD= 0 mV
T = 0.1 K
VG1&G2 (V)
-1.5
-2.5
-2.0
νQPC
νBULK
νBULK

## Slide 13: Fractional edge channels
Weak B-field: spin splitting
Intermediate B-field: integer and fractional edge-channels
Strong B-field & low density: Interference and localisation
 Filter for (fractional) edge channels
VG1&G2 (V)
-2.7
-2.5
-2.1
-1.7
-1.5
-2.3
-1.9
QPC4
T = 0.1 K
VSD = 0 mV
νQPC
0
2
3
1
0
1
0
1
νQPC
νQPC
B┴= 3.3 T
νBulk= 4
1
2
3
B┴= 6.8 T
νBulk= 2
B┴= 12.8 T
νBulk= 1
1
4/3
5/3
2/3
1

## Slide 14: Localized Edge Channels  Coulomb Blockade
νQPC = 1
400 nm
B (T)
VPG (V)
-2.196
-0.60
ΔB = 1.9 mT
ΔVPG = 7.7 mV
-2.205
-0.66
1.65 nA
1.67 nA
ΔVG: adjust charge of localized edge channel
ΔB: redistribute electrons between edge channels see also: Y. Zhang et al., Phys. Rev. B 79, 241304 (2009)
N. Ofek et al., PNAS 107, 5276 (2010)
B. I. Halperin et al., Phys. Rev. B 83, 155440 (2011)
νbulk = 2
νbulk = 2
νQPC = 1
B (T)
VPG (V)
-1.101
-0.60
ΔB = 1.0 mT
ΔVPG = 7.2 mV
-1.107
-0.65
3.01 nA
3.05 nA
νQPC = 2
νbulk = 4
νbulk = 4
νQPC = 2
400 nm

## Slide 15: Coulomb-Coupled Edge Channels
νQPC ≈ 0, νbulk = 2
400 nm
ΔB = 3.0 mT
B (T)
-2.112
-2.1
VPG (V)
-0.60
-0.66
ΔVPG = 6.0 mV
0 pA
50 pA
ΔVG or ΔB: redistribute electrons between edge channels
High current if outer edge channel in resonance
Analogy to capacitively coupled double quantum dot
VPG (V)
-0.54
-0.66
ISD (pA)
0
50
ISD (pA)
0
50
B (T)
-2.102
-2.111

## Slide 16: Coulomb-Coupled Edge Channels
νQPC ≈ 0, νbulk = 2
400 nm
ΔB = 3.0 mT
B (T)
-2.112
-2.1
VPG (V)
-0.60
-0.66
ΔVPG = 6.0 mV
0 pA
50 pA
ΔVG or ΔB: redistribute electrons between edge channels
High current if outer edge channel in resonance
Analogy to capacitively coupled double quantum dot
νQPC ≈ 0, νbulk = 4
400 nm
ΔB = 1.5 mT
B (T)
-1.058
-1.05
VPG (V)
-0.50
-0.56
ΔVPG = 6.1 mV
0 pA
100 pA
see also:
P. L. McEuen et al., Phys. Rev. Lett. 66, 14 (1991)
N. C. van der Vaart et al., Phys. Rev. Lett. 73, 320 (1994)
T. Heinzel et al. , Phys. Rev. B 50, 20 (1994)

## Slide 17: Analogy: Double Quantum Dot
400 nm
n
m
n-1
m
n+1
m-2
n
m-1
n
m-2
n+1
m-1
n-1
m-1
VG
B
Capacitor network model
Reconstuct hexagon pattern from peak positions
B-field axis tilted  edge state radii differ by ≈ 60 nm
ΔB = 3.0 mT
ΔVPG (shifted)
ΔB = 1.5 mT
ΔVPG (shifted)
νQPC ≈ 0, νbulk = 2
νQPC ≈ 0, νbulk = 4
CL
ν = 1
C1-PG
C2-PG
PG
C1-2
ν = 2
ν = 0
E
x
y

## Slide 18
Charge Detection
400 nm
Capacitively coupled QPC
Detect transferred charge
Future studies: Can we detect fractional charge?
QPC
t (s)
IQPC(pA)
VG (V)
# of Events
760
10
800
0
-760
-820
0
600
S. Baer, C. Rössler et al., submitted

## Slide 19: Summary & Outlook
Quantum Point Contacts in Ultra Clean Electron Systems
Extract shape parameters
Many-body effects
  0.7 anomaly
  Enhanced spin-splitting
  Fractional edge channels
Interferometry
Interplay between Coulomb-blockade and Aharonov-Bohm effect
Charge detection in the QHE-regime
S. Baer, C. Rössler et al., submitted (2012)
C. Rössler et al., New J. Phys. 12, 043007 (2010)
C. Rössler et al., New J. Phys. 13, 113006 (2011)
Scanning Gate Microscopy
Imaging interference in real space
Talk of Aleksey Kozikov on Friday
500 nm
S. Schnez, CR et al., Phys. Rev. B 84, 195322 (2011)
A. A. Kozikov , C. Rössler et al., submitted (2012)